Investigation of effect of microalloying elements and hot rolling parameters on the strength of low-carbon steels

Aleksei Dagman

Novolipetsk Steel, Lipetsk, Russia, dagman_ai@nlmk.com

+7-4742-444348

ABSTRACT:

Presently steel products manufacturers focus on searches of influence of chemical composition and parameters of thermal-deformation treatment of metal on the formation of microstructure and system of nanosized phase precipitates of different types and, ultimately, the obtained mechanical properties.

The report presents one of the solutions to this problem. The influence of structural state characteristics on the mechanical properties of low-carbon hot-rolled Mo-containing steels of three microalloying systems, Ti-Mo, V-Mo, and Nb-V-Mo, was studied, depending on the temperatures of the rolling end and coiling of the strip. To analyze the type and quantity of nanosized phase precipitates, the transmission electron microscopy method and thermodynamic calculation of the temperature dependences of the equilibrium phase composition of the studied steels were used.

It was found that the highest values ​​of strength and ductility are exhibited by steels microalloyed with titanium and molybdenum with a single-phase ferritic microstructure. In this case, the metal matrix consists of ferrite of two morphological types: polygonal and block. The high level of strength is achieved due to precipitation hardening caused by a large number of nanoscale interphase precipitates. This was facilitated by relatively high temperatures of the rolling end (860-880 ºC) and coiling (570-590 ºC) and a molybdenum concentration of  ≥ 0.16 wt.%.

BIOGRAPHY: 

Aleksei Dagman

PhD (Tech.)

Expert discipline lead, Technology R&D

Novolipetsk Steel (NLMK), Russia

He has industrial experience in the development and improvement of integrated metallurgical production technologies in the production of structural, pipe, automotive and electrical steels.

The number of publications is more than 80.

Area of interest: production of low-carbon, low-alloy, high-strength steels.

Phone: 7-4742-444348

E-mail: dagman_ai@nlmk.com